# Learning Objectives

Lecture 1:

- Understand why the study of biomaterials is an important aspect of the educational background of the biomedical engineer;

- Understand what a biomaterial is;

- Be able to differentiate between the different general applications of biomaterials;

- Provide specific examples of classes of products on the basis of application; and,

- Be able to differentiate between the scientific and the regulatory definition of biomaterials.

Lecture 2:

- Know what government body regulates medical devices;

- Be able to differentiate between the various classes of medical devices from a regulatory perspective and be able to provide examples of each class of device;

- Understand what is meant by biocompatibility testing and why it is a necessary consideration in the manufacture of medical devices;

- Understand what is meant by the phase, “biological response to contact with materials”;

- List the different procedures used to test biocompatibility;

- Become aware of the Society of Biomaterials, of the various professional journals; and relevant websites;

- Be able to broadly differentiate between the different classes of biomaterials;

- Explain what a ceramic is and how they are used clinically;

- Explain what a metal is and how they are used clinically;

- Explain what a polymer is and how it is used clinically;

- Differentiate between the concepts of bioenertness and bioactivity; and

- From a biomedical device standpoint, know what is generally required of a biomaterial to be incorporated within a biomedical device

Lecture 3:

- Differentiate between the concepts of inertness and bioactivity;

- From a biomedical device standpoint, know what is generally required of a biomaterial to be incorporated within a biomedical device;

- Be able to describe what a polymer is and provide examples of how they are used in biomedical devices;

- Understand what distinguishes polymers for other compounds;

- Describe how carbon chain length is related to the physical state, properties and uses of alkanes;

- Understand the fundamental nomenclature of polymeric structure;

- Describe what is meant by the terms “homopolymer, heteropolymer and vinyl polymer;

- Understand how to represent various common polymers by representing the meric unit in chemical shorthand and known the common abbreviation for the following polymers: polyethylene (PE); polypropylene (PP), polystyrene (PS), polyvinylchloride (PVC); polytetraflouroethylene (PTFE), polyacrylic acid (PAA); poly(methylmethacrylate) (PMMA); poly(vinylacetate) (PVAc); poly(vinylidene dichloride) (PVDF); Poly(ethylene oxide) (PEO); poly(caprolactam) (nylon);  poly(hexamethylene adipamide) (Nylon 6,6); poly(ethylene terephthalate) (PET); poly(carbonate); poly(dimethylsiloxane) (PDMS); and poly(methyl styrene);

- Understand what is meant by the term polymer “conformation”;

- Be able to provide a sketch of the randon coil model of polymer structure;

Lecture 4

- What is meant by the term polyelectrolyte;

- In general terms, what makes one polymer different from another;

- In general terms, how does increases in polymer molecular weight affect mechanical and chemical properties;

- Draw a graph of the general relationship of increasing molecular weight on stiffness and strength (can you explain the relationship at the level of polymer chain interaction);

- Differentiate between the terms hydrophilicity and hydrophobicity;

- Provide two examples of different types of polymerization reactions;

- What is meant by the term condensation reaction;

- Explain what is meant by the term monodisperse polymer;

- How are synthetic polymers different from natural polymers such as proteins;

- How does number average molecular weight differ from weight average molecular weight;

- What is polydispersity mean and how does one calculate polydispersity;

- List several ways to experimentally determine a polymers molecular weight;

Lectures 5-7 -Wound healing response

- Describe what is meant by the term wound healing continuum;

- List the important major events that take place in the typical wound healing process;

- What is meant by the term “hemostasis”;

- Describe in order the 4 major events that occur following the loss of vascular integrity;

- Describe what is meant by the term “blood coagulation cascade;

- What are serine proteases and what role do they play in blood clotting;

- What is meant by the term “platelet activation”;

- What is the major difference of the intrinsic and extrinsic coagulation cascades;

- Describe what is meant by the final common pathway;

- In general, how does the implantation of a biomaterial influence the wound healing process;

- What initiates the inflammatory response?;

- What is meant by the term provisional matrix?;

- How does platelet degranulation influence wound healing;

- What are the major cytokines released by platelets and how do they affect the wound healing process?;

- What is the TGF-beta and how does it affect the wound healing cascade;

- Where do macrophages come from?;

- What is meant by the term angiogenesis and what factors stimulate new blood vessel formation?;

- What role do fibroblasts play in wound healing?

- Describe what is meant by the term granulation tissue;

Surface Properties of Biomaterials lecture 8

- What defines a surface, an interface?

- List and describe characteristics that are unique to surfaces

- Give an example of surface dynamics

- Describe excess surface free energy

- Define the thermodynamic concept of surface energy

- Define the work of adhesion and cohesion

- Interpret (with words) the Young-Laplace equation

- Interpret the Gibbs-Kelvin equation (compare to Y-L)

- Derive the Young-Dupre equation for a liquid drop on a rigid surface

- Summarize the strong and weak intermolecular forces

- What distinguishes Van der Waals interactions?

- What two forces are combined in DLVO theory?

Surface Characterization lecture 9

- Define the probe, sample type, and signal for ESCA, SIMS, contact angles (CAs), and SPM

- Describe the working principle of ESCA, SIMS, CAs, and SPM

- What determines surface sensitivity?

- Derive the Young-Dupre equation for a captive bubble on a rigid surface

- What can be varied in a contact angle experiment?

- Describe the Zisman CA method

- Describe the Fowkes CA method

- List four potential sources of error in CA experiments

- Contrast photoemission and Auger emission in terms of ESCA signal

- How can you increase depth sensitivity for ESCA /SIMS?

- How is the imaging mode of ESCA / Auger / SIMS like SPM?

- List and describe the three most common AFM modes

- What is “functional imaging” with the AFM?

Protein and Surface Interaction lecture 10

- Describe structural features of proteins that affect their adsorption to surfaces

- Contrast adsorption and absorption

- Is protein adsorption energetically favorable?

- Is protein adsorption reversible?

- What are the driving forces for protein / cell adsorption?

- Describe protein dynamics following adsorption

- Describe the Langmuir isotherm and its major assumptions

- Draw the kinetic model for Langmuir adsorption

- Describe the “Vroman effect”

- Describe the low critical energy hypothesis

- Describe the low interfacial energy hypothesis

- What is the effect of water as a solvent during protein adsorption?

- Describe one example where protein adsorption to an unmodified material leads to a significant biological response

- Why is the end result of implantation generally fibrous encapsulation?

- Describe three methods to pattern a surface (pattern with what material?)

- Describe the effect of PEO grafted chains on protein adsorption.

Lectures 11 & 12-(Inflammation Part I and II)

- In general terms describe what is meant by the terms “complement” and complement cascade”

- With regard to biomaterials, describe want is meant by the cellular and humoral arms of the immune system;

- Provide a diagrammatic description of the complement system;

- How does the complement cascade differ from the coagulation cascade; ;

- List several important complement mediators and their functions;

- Provide practical examples of devices that would be expected to activate the inflammatory response;

- Describe the consequences of chronic or prolonged inflammation;

- Clinically speaking, describe how one might think of inhibiting the process