Lecture 22-23 (Hollow Fibers Biomaterials in Nephrology)

- Within the context of biomaterials, what is meant by the term “hollow fiber”;

- List several important biomedical applications of hollow fibers;

- What is meant by the terms “semipermeable or selectively permeable”;

- How are hollow fibers used in nerve repair;

- Within the context of cell encapsulation, what is meant by the term “immunoisolation”;

- What is meant by the term “phase inversion”;

- How are hollow fibers made;

- What types of reagents are required for fabricating a hollow fiber;

- What is meant by the term “ annular spinneret”;

- How is the perm-selective skin of a hollow fiber created;

- Why do many types of hollow fibers have an anisotropic wall architecture;

- What does the ultra-topography of the inner skin look like and why does it have this characteristic structure;

- How does one characterize the sieving or filtration properties of a hollow fiber membrane;

- What is meant by the term “Molecular Weight Cut-off (MWCO);

- What is meant by the term hindered diffusion;

- Describe how a hemodialyzer is constructed and how it functions;

- What are the primary issues that determine hemodialysis biocompatibility;

- What is the chemical nature of Cuprophane;

- What are the clinical symptoms most frequently observed after the use of cuprophan heomdialyzers;

Lecture 24 (Hydrogels)

- Provide a complete definition of the term “hydrogel”;

- Describe the various chemical schemes that can participate in the constructuion of a hydrogel network;

- What is meant by the phrase “hydrogel water content can vary from 10-95%”?;

- How is swell behavior characterized empirically?;

- What is meant by the term “supramacromolecule”?

- What two characteristics determine the size of a swollen hydrogel network?;

- What is meant by the term “xerogel”?;

- What is the chemical nature of chitosan and where is ti derived?;

- How are xerogels and hydrogels used in drug delivery applications;

- List five naturally occurring hydrogels;

- List the functions of biological hydrogels;

- List five synthetic hydrogels;

- What are the common chemical attributes of hdrogels?

- What is meant by the term “polyelectrolyte hydrogels’ and how are they used?;

- Differentiate between hylauronic acid and alginic acid in terms of structure and function;

- Describe a scheme for encapsulating cells in a biocompatible hydrogel coating using polyelectrolytes;

Lecture 25-(Applications in Opthalmology)

- Describe the chemical nature of “polyacrylates”;

- How are poly(acrylates) synthesized;

- Describe four significant events in the historical development of contact lens;

- Describe why the original PMMA contact lens were not as biocompatible as pHEMA lens;

- Differentiate pMMA and pHEMA;

- List the properties that make pHEMA useful as a contact lens material;

- List three ways by which contact lens can be fabricated;

- What is a cataract;

- What is meant my the term “IOL”;

- List the common materials used for making intraocular lens;

- What was the firs materials used for making IOL’s and why was it chosen/;

- What are the most common complications with IOL’s;

- What animal model is generally used in the development of IOL’s and why is it used;

- What is meant by the term “calification”;

- What type of additives are added to IOL’s to protect the retina;

- What are the two major causes of lens opacification?;

- What is meant by a “3-pience lens”;

- What is the chemical nature of the calcification;

Lecture 26-28 (Metals-Parts I, II & Applications)

- On a broad level, list the various types of biomaterials;

- From an engineering perspective, what are the advantages of using metals as biomaterials;

- List 4 applications of metals and provide specific examples of devices and their uses;

- List several physical properties that are characteristics of metals;

- List several chemical properties that are characteristics of metals;

- Provide a simple chemical definition of metals;

- List three common lattice types and describe how they are related to mechanical properties;

- What is meant by the statement “the details of the processing can strongly affect the mechanical properties of a metal”;

- What is meant by the term “grain formation”;

- From a structural perspective, what is meant by the term “phase”;

- Describe two defects in lattice architecture and provide an explanation of how they affect mechanical behavior of the solid;

- What is meant by the term “fatigue failure”;

- How are the mechanical properties of the metal related to its internal structure?;

- Describe two methods of increasing the strength of a metal;

- What is meant by the term “alloy”;

- What are the two principle types of alloys;

- List several important alloys and their uses;

- What is meant by the term “strain hardening”;

- List three common metals used as biomaterials;

- For long term use, What metals are preferred and why;

- Describe the principal components of the total artificial knee and provide a list of materials;

- Describe the major cause of revision surgery with the TKR

Lecture 29 (Ceramics and glasses)

- Differentiate the terms “ceramic and glass”;

- How do metals compare with ceramics in terms of physical properties?;

- What are the generally accepted advantages and disadvantages of using ceramics as biomaterials?;

- List several orthopedic applications of ceramics;

- List several dental applications of ceramics;

- What are the four most commonly sued ceramics?;

- What is meant by the term “osteintegration” and how is it achieved;

- Describe the various possible conceptual interactions of ceramics and tissue;

- Describe a generic processing scheme for processing a ceramic implant;

- List two commonly used structural bioceramics;

- Provide two common failure mechanisms of the total artificial hip;

- What is the composition of dental porcelain?;

- What is meant by the term “calcium phosphates”;

- What is the inorganic component of bones and teeth?;

- List several ways that calcium hydroxyapatite is in the biomedical device industry;

- What is meant by the term “bioceramic coating”? and, what is a rationale for their use?;

- What is meant by the term “tissue engineering”;

- Describe a tissue engineering scheme to replace bone in a defective mandible>

Lecture 30 (Adhesives and Sealents)

- Define the terms “adhesion” and “adhesive”;

- What is meant by the term “sealant”;

- How are adhesives and sealants used as biomaterials?;

- List several ways that can be used to classify adhesive materials;

- As an design engineer, what generally needs to be considered in the selection of a particular adhesive?;

- List the factors that determine the breaking strength of an adhesive joint;

- List four common adhesives;

- Differentiate between different bonding mechanisms;

- What is meant by the term “surface treatment” and how do the various treatments increase adhesive bond strength;

- Differentiate between the various terms used in failure analysis;

- Differentiate between the two major types of adhesives and provide an example of each;

- What is meant by the term “ light cured system”;

- Describe some of the fundamental characteristics of light cure adhesives;

- What are some of the typical applications of light cure adhesives;

- From an biomedical engineering perspective, what are the benefits of adhesives;

- From an biomedical engineering perspective, what are the limitations of adhesives;

- On the basis of their limitations, differentiate between cyanacrylate adhesives, light cured acrylate adhesives; epoxy adhesives; and polyurethane adhesives;

Lecture 31 (Biomaterials in Dentistry)

- What is meant by the term “adhesive dentistry”?;

- Describe how sealants are used;

- What is a glass ionomer cement and how is it used;

- Glass ionomer restorations are bacteriostatic- explain;

- Glass iomers are composites-explain;

- What is the most common dental resin used in composite restorations?;

- What is meant by the term “inorganic filler”?;

- How are restorations like “sustained release” formulations?

Lecture 32-33 (biodegradable materials)

- Using graphical representation, show what is meant by the term “polymer degradation”;

- Provide a rationale for the use of degradable materials in orthopedic medicine;

- List several advantages for the use of biodegradable implants;

- Provide four general structural formulas depicting degradable functional groups;

- Be able to identify the most likely hydrolytic sites in common structural formulae;

- List several natural and several synthetic degradable polymers used in medical applications;

- What are the advantages of synthetic degradable polymers over natural ones?;

- Outline the synthesis of poly(glycolic acid);

- With a graph, describe how varying the ratio of PGA to PLA influences the time of degradation of the co-polymer;

- What are the two most common mechanisms of biodegradation?;

- With respect to biomedical device design, differentiate between surface and bulk degradation;

- List the most important factors that affect the behavior of degradable polymers;

- List five common methods for studying polymer degradation;

- What would a comparison of Tgs tell you about the degradation of two different PGLA copolymers;

- How is average molecular weight influenced over time?;

- What methods would you use to study how average molecular weight is affected over time;

- List several medical specialties which make use of degradable materials and provide specific examples of their applications;

Lecture 34 (TE and Biomaterial Processing)

- What is meant by the term “tissue engineering scaffold”;

- Describe how a porous scaffold would be prepared using the solvent casting method;

- Differentiate between the terms particle leaching, ball leaching and filament leaching;

- What are the major consideration when using a leaching process to create a porous scaffold or substrate;

- What are the major methods for creating porous tissue engineering scaffolds;

- What is the difference between melt spinning and electrospinning processes;

- Describe a simple way to create a scaffold using thermoplastic filaments;

- In the future, how is it envisioned that imaging can be integrated into the manufacture of tissues for therapeutic use?;